Course Outline

Title:	Properties of Materials	Course Number:	ENGR-231

Credits:	4

Date:	November 2012

Institution:	Clackamas Community College

Outline Developed by:	Engineering Science department, Eric Lee

Type of Program:	Lower Division Collegiate

Course Description:

An introduction to materials science, a field that describes the behavior of materials by utilizing principles of chemistry and physics to engineer new materials and predict their resultant properties. The course will focus on describing the microscopic physical and chemical structure of materials and relating that structure to the macroscopic thermal, electrical, and mechanical properties. The course will also cover the connection between atomic/crystal structure and materials processing.

Student Learning Outcomes:

Upon successful completion of this course, students should be able to:

- predict basic physical properties of materials based on their elemental composition and type of chemical bonding, (SC1, SC2)

- describe the compositions, phases, and microstructure of binary solid systems after heat treatment based on the binary phase diagram; (SC1, SC2)

- characterize the kinetics of phase transformations in metal alloys by applying the principles of solid state diffusion and nucleation theory, (SC1, SC2)

- interpret the nomenclature of Bravais lattices and Miller indices to describe the structure of crystalline materials. (MA1, MA2, SC1, SC2)

Length of Course:	33 lecture hours, 33 lab hours

Grading Method:	Letter grade (A-F) or Pass/No pass

Prerequisites: 	Pass CH-221

Co-requisites:	None

Recommended:	None

Required:	None

Major Topic Outline

- Atomic Structure and Bonding

- Structure of Crystalline Solids

- Diffusion

- Phase Diagrams

- Properties of Materials

Composites

CCC AAOT/ASOT GENERAL EDUCATION OUTCOMES 	Course Title and Number:     ENGR-231

COURSE OUTLINE MAPPING CHART	Properties of Materials

Mark outcomes addressed by this course:

- Mark “C” if this course completely addresses the outcome. Students who successfully complete this course are likely to have attained this learning outcome.

- Mark “S” if this course substantially addresses the outcome. More than one course is required for the outcome to be completely addressed. Students who successfully complete all of the required courses are likely to have attained this learning outcome.

- Mark “P” if this course partially addresses the outcome. Students will have been exposed to the outcome as part of the class, but the class is not a primary means for attaining the outcome and assessment for general education purposes may not be necessary.

As a result of completing the AAOT /ASOT general education requirements, students will be able to:

| WR: Writing Outcomes |  |
| --- | --- |
| 1. Read actively, think critically, and write purposefully and capably for academic and, in some cases, professional audiences. |  |
| 2. Locate, evaluate, and ethically utilize information to communicate effectively. |  |
| 3. Demonstrate appropriate reasoning in response to complex issues. |  |
| SP: Speech/Oral Communication Outcomes |  |
| 1. Engage in ethical communication processes that accomplish goals. |  |
| 2. Respond to the needs of diverse audiences and contexts. |  |
| 3. Build and manage relationships. |  |
| MA: Mathematics Outcomes |  |
| 1. Use appropriate mathematics to solve problems. | P |
| 2. Recognize which mathematical concepts are applicable to a scenario, apply appropriate mathematics and technology in its analysis, and then accurately interpret, validate, and communicate the results. | P |
| AL: Arts and Letters Outcomes |  |
| 1. Interpret and engage in the Arts & Letters, making use of the creative process to enrich the quality of life. |  |
| 2. Critically analyze values and ethics within a range of human experience and expression to engage more fully in local and global issues. |  |
| SS: Social Science Outcomes |  |
| 1. Apply analytical skills to social phenomena in order to understand human behavior. |  |
| 2. Apply knowledge and experience to foster personal growth and better appreciate the diverse social world in which we live. |  |
| SC: Science or Computer Science Outcomes |  |
| 1. Gather, comprehend, and communicate scientific and technical information in order to explore ideas, models, and solutions and generate further questions. | P |
| 2. Apply scientific and technical modes of inquiry, individually, and collaboratively, to critically evaluate existing or alternative explanations, solve problems, and make evidence-based decisions in an ethical manner. | S |
| 3. Assess the strengths and weaknesses of scientific studies and critically examine the influence of scientific and technical knowledge on human society and the environment. |  |
| CL: Cultural Literacy Outcome |  |
| 1. Identify and analyze complex practices, values, and beliefs and the culturally and historically defined meanings of difference. |  |
| IL: Information Literacy Outcomes |  |
| 1. Formulate a problem statement. |  |
| 2. Determine the nature and extent of the information needed to address the problem. |  |
| 3. Access relevant information effectively and efficiently. |  |
| 4. Evaluate information and its course critically. |  |
| 5. Understand many of the economic, legal, and social issues surrounding the use of information. |  |

# Endnotes

“Arts and Letters” refers to works of art, whether written, crafted, designed, or performed and documents of historical or cultural significance.

Must be embedded in a course that meets the outcomes for Arts and Letters, Social Science, or Science/Computer Science.

Must be embedded in the general education required Writing courses     Revised 2010-2011 to reflect Statewide AAOT outcomes